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Hydroxypropyl Starch Ether

General 

Hydroxypropyl starch ether ZX-SC-02 is hydroxypropyl starch ether (HPS) which is a white fine powder made from natural plants. Its molecular formula is (C6H10O5) n and ZX-SC-01 is a starch substituent ether produced by the reaction of hydroxyl groups in starch molecules with reactive substances, including hydroxypropyl starch,  carboxymethyl starch,  and cationic starch, etc.

Composition




(C6H10O5) n
Product properties
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Appearance						             	White powder
Odor								            Odorless
Physical state							            Powder
PH 								                9 - 11
Solubility						                    Dissolves in cold water
Fineness 							            ＜ 350 micron   
Viscosity							                400 - 1200 mPa.S
Moisture							                ＜ 5%

Application




Application range

Hydroxypropyl starch ether ZX-SC-02 can improve the performance of dry mortar based on cement and gypsum. It has a very good rapid thickening ability, and a very low addition amount in building materials It can achieve high results such as improving  the material's own anti-sagging ability, having good lubricity,  improving the operation performance of the material, and making the operation more slippery.

Packing

25 kg nylon woven bag or composite kraft paper bag, and package upon customer’s request.

Storage and Transportation

Hydroxypropyl starch ether ZX-SC-02 should be stored in a ventilated, cool and dry environment. Storage period is generally one year. It can still be used after the inspection.

Hydroxypropyl starch ether ZX-SC-02 is non-dangerous goods. In the process of transportation, it should prevent the sunlight and rain and should not be transported with spontaneous combustion, strong oxidant, strong acid.

Safety and handling 


Wherever dust or melt fume is produced, provide the proper exhaust ventilation. After handling, properly wash your hands. Put on gloves and appropriate safety gear.

The Material Safety Data Sheet provides further details on first aid, fire safety precautions, transportation information, and laws. It can be obtained upon request.


